[image: image1.jpg]BEBON

BebonChina.com

3




[image: image1.jpg]                                      Henan BEBON international co.,ltd

Steel for Boilers and Pressure Vessels

Pressure vessel and boiler quality steel are commonly used throughout the oil industry (including inshore and offshore), the petrochemical industry and the gas production industry. 

Boiler steel plate has good strength, it can be made of boilers and components to withstand a certain long-term high temperature stress; Boiler steel plate has good toughness and low effectiveness of the tendency in the use of bending, curling, deformation processing such as cold, after more prolonged storage and use remains a good toughness; Boiler steel plate also has good weldability and resistance to intergranular corrosion. For the manufacture of boiler drum, beams and wall panels. 

Steel for Pressure Vessels contains:Low-temperature low-alloy steel for pressure vessel, normal temperature pressure uses the steel,Quenched and tempered high strength steel plates for pressure vessels.  

The delivery condition of Boilers and Pressure Vessels Steel are: Normalize, annealing,tempering,TMCP,PWHT, impact test,Q&T.

The main steel grade of Pressure vessel and boiler quality steel are :

EN 10028-2:  P235 GH, P 265 GH, P 295 GH, P 296 GH, P 355 GH

EN 10028-3: P 275 N, P 275 NHP, 275 NL 1, P 275 NL 2, P 355 N, P 355 NH, P 355 NL 1, P 355 NL 2

DIN17165 : HI , HII, 17 Mn 4, 19 Mn 8

DIN17102: St E 255, W St E 255, T St E 255, E St E 255, St E 285, W St 285, T St E 285, E St E 285, St E 315, W St 315, T St E 315, E St E 315.  St E 355, W St E 355, T St E 355, E St E 355.

JIS G 3115: SPV 235, SPV 315 ,SPV 355

JIS G 3103: SB 410 ,SB 450, SB 480

ASTM: A 285gr.A/B/C,  A299, A441, A442gr.55/60, A455,  A515gr55/60/65/70,  A516gr55/60/65/70, A 537CL1/2/3, A 612, A 622grA/B/C.  A737grB/C. 

	Europe
	Germany DIN
	franch
	Japan JIS G
	USA

	EN 10028-2
	EN 10028-3
	EU 113
	17135
	17165
	17102
	NFA36205
	3115
	3103
	ASTM

	P235 GH
	
	FeE255KG KW,KT
	A St 35
	HI
	St E 255
	
	SPV 235
	SB 410
	A 285gr.A,B,C

	
	
	
	
	
	W St E 255
	
	
	
	

	
	
	
	
	  
	T St E 255
	A 37 CP, AP,FP
	
	
	A299

	
	
	
	
	
	E St E 255
	
	
	  
	A441gr.55,60

	P 265 GH
	P 275 N
	FeE285KG,KW,KT
	A St 41
	HII
	St E 285
	A 42 CP,AP,FP
	
	
	

	
	P 275 NH
	
	
	
	W St 285
	
	
	
	A442 gr.55,60

	
	P 275 NL 1
	
	
	
	T St E 285
	
	
	
	A455

	
	P 275 NL 2
	
	
	
	E St E 285
	
	
	
	

	P295 GH
	
	FeE315KG,KW,KT
	A St 45
	17 Mn 4
	St E 315
	  A 48 CP,AP,FP
	SPV 315
	SB450
	A515gr.55,60,65,70

	
	
	
	
	
	W St E 315
	
	
	
	

	
	
	
	
	
	T St E 315
	
	
	
	A516gr.55,60,65,70

	
	
	
	
	
	E St E 315
	
	
	
	

	P 355 GH
	P 355 N
	FeE355KG,KW,KT
	A St 52
	19 Mn 8
	 St E 355
	A 52 CP,AP,FP
	SPV 355
	SB 480
	A 537class 1

	
	P 355 NH
	
	
	
	W St E 355
	
	
	
	

	
	P 355 NL1
	  
	
	
	T St E 355
	
	
	
	A 612

	
	P 355 NL2
	  
	
	
	E St E 355
	
	
	
	A 622gr.A,B,C

	
	
	
	
	
	
	
	
	
	A737gr.B,C


[image: image2.jpg]


Bebon steel  ——  The most professional exporter on weathering resistant steel
Tel:0086-371-86151527                                         E-mail:bb@bebonchina.com                           

Fax: 0086-371-86011881                                        MSN:bebonchina@hotmail.com                                 Skype：bebonchina                                             Web:http://www.shipbuilding-steel.com

                                                               http://www.bebonchina.com 

Oficina Dir: 2801 B# Intermational enteprise center Zhengzhou city in China.

