[image: image1.jpg]BEBON

BebonChina.com

3




[image: image1.jpg]                                      Henan BEBON international co.,ltd

Steel for gas cylinders and gas vessels

DIN, NFA, EN, UNI, JIS  Steel for gas cylinders and gas vessels，Steel for gas cylinders and gas vessels plate, Steel for gas cylinders and gas vessels sheet, Steel for gas cylinders and gas vessels coil, Steel for gas cylinders and gas vessels supplier

Steel for gas cylinders and gas vessels description

Steel for gas cylinders and gas vessels, just as its name implies, is the Hot-rolled structural steel plate and sheet for making gas cylinders and gas vessels. Steel for gas cylinders and gas vessels has excellent properties for deep drawing and welding and meets all the performance requirements for this application.

Steel for gas cylinders and gas vessels Application

These steel grades are characterised by a minimum yield strength of 245 - 355 MPa and by good weldability. The user of these steel grades must make sure that his calculation, design and processing methods are appropriate for the material. The steel grades of this series are used for manufacturing gas cylinders by welding cold-formed parts together and normalizing the finished cylinder.

The main grade of Steel for gas cylinders and gas vessels are :

Material #: 1.0111, 1.0243, 1.0437, 1.0557

EN 10120: P245NB, P265NB, P310NB, P355NB

DIN 17155: H I, H II, 17 Mn 4, 19 Mn 6

NFA 36-211: BS 1/2/3/4

UNI 7355: Fe E 24 KR, Fe E 27 KR, Fe E 31 KR, Fe E 35 KR

BS 5045: Type A/B/C/D

UNE 36129: AE 235 KR, AE 265 KR, AE 345 KR

JIS G3116:  SG 255 , SG 295, SG 325, SG 365.

Steel for gas cylinders and gas vessels equivalent grades

	Material #
	EN 10120
	DIN 17155
	NFA 36-211
	UNI 7355
	BS 5045
	UNE 36129
	JIS G3116

	1.0111
	P245NB
	H I
	BS 1
	Fe E 24 KR
	Type A
	AE 235 KR
	SG 255

	1.0243
	P265NB
	H II
	BS 2
	Fe E 27 KR
	Type B
	AE 265 KR
	SG 295

	1.0437
	P310NB
	17 Mn 4
	BS 3
	Fe E 31 KR
	Type C
	AE 345 KR
	SG 325

	1.0557
	P355NB
	19 Mn 6
	BS 4
	Fe E 35 KR
	Type E
	　
	SG 365


Steel for gas cylinders and gas vessels Supply Size

Thickness: -

Mill finish: 1.47 - 5.00mm

Pickled: 1.50 - 5.00mm

Width: -

Mill finish: 710 - 2070mm

Pickled: 735 - 2070mm

Steel for gas cylinders and gas vessels Delivery state

Hot Rolled, Cold Rolled, Normalized, Quenched, Tempering, Thermal Mechanical Control Process (TMCP), Electroslag Remelting Technical, HIC test.

Steel for gas cylinders and gas vessels Services

Cutting, Painting, shot blast, and The third party inspection in DNV, BV, LR, GL, ABS, CCS , SGS, and others in super thick ship steel plate.

Steel for gas cylinders and gas vessels Chemical composition

	Grade
	C
	Si
	Mn
	P
	S
	N 2)
	Altotal1)
	Ti
	Nb

	
	max.
	max.
	min.
	max.
	max.
	max.
	min.
	max.
	max.

	P245NB
	0,16
	0,25
	0,30
	0,025
	0,015
	0,009
	0,020
	0,03
	0,050

	P265NB
	0,19
	0,25
	0,40
	0,025
	0,015
	0,009
	0,020
	0,03
	0,050

	P310NB
	0,20
	0,50
	0,70
	0,025
	0,015
	0,009
	0,020
	0,03
	0,050

	P355NB
	0,20
	0,50
	0,70
	0,025
	0,015
	0,009
	0,020
	0,03
	0,050


1) The aluminium content may in part be replaced by ≤ 0,050 % Nb and /or ≤ 0,03 % Ti.
2) With a ratio of Altotal / N ≥ 2,2 or if Nb or Ti are added, the nitrogen content 
    may be ≤ 0,012 %. 
Steel for gas cylinders and gas vessels Mechanical properties1)
	Grade
	Min. yield strength
	Tensile strength
	Min. total elongation [%]

	 
	MPa
	MPa
	L0 = 80 mm
	L0 = 5,65 √S0

	 
	 
	 
	e2) < 3 
	e2) ≥ 3

	P245NB
	245
	360 - 450
	26
	34

	P265NB
	265
	410 - 500
	24
	32

	P310NB
	310
	460 - 550
	21
	28

	P355NB
	355
	510 - 620
	19
	24


1) Transverse samples
2) Nominal thickness e [mm] 
Bebon International is a global steel supply and stockholding company. Partnerships integrating the resources of the China’s most technically advanced steel mills enable Bebon International to provide a single competitive source for the distribution of steel products worldwide. 

Bebon International offer premium quality Steel for gas cylinders and gas vessels Plates. These Steel for gas cylinders and gas vessels plates have consistent and controlled properties, designed for withstanding the high pressure for gas cylinders and gas vessels.

Bebon International has one of the widest steel plate product ranges in the world. Whether you are a designer, contractor or fabricator you will find our product range both modern and extensive. Steel for gas cylinders and gas vessels offered by Bebon is in very high quality to support the requirements of those engaged in large projects.

[image: image2.jpg]


Bebon steel  ——  The most professional exporter on weathering resistant steel
Tel:0086-371-86151527                                         E-mail:bb@bebonchina.com                           

Fax: 0086-371-86011881                                        MSN:bebonchina@hotmail.com                                 Skype：bebonchina                                             Web:http://www.shipbuilding-steel.com

                                                               http://www.bebonchina.com 

Oficina Dir: 2801 B# Intermational enteprise center Zhengzhou city in China.

