[image: image1.jpg]BEBON

BebonChina.com

3




[image: image1.jpg]                                      Henan BEBON international co.,ltd

Steel for large diameter pipes

DIN, EN,API  Steel for large diameter pipes，Steel for large diameter pipes plate, Steel for large diameter pipes sheet, Steel for large diameter pipes coil, Steel for large diameter pipes supplier

Steel for large diameter pipes description

Steel for large diameter pipes, just as its name implies, is the Hot-rolled structural steel plate and sheet for making Large-diameter pipe (25 centimeters (10 inch) or greater) may be ERW, EFW or Submerged Arc Welded ("SAW") pipe. Steel for large diameter pipes has excellent properties for welding and meets all the performance requirements for this application.

Steel for large diameter pipes Application

These steel grades are characterised by a minimum yield strength of 245 - 355 MPa and by good weldability. The application of these steel plates is mainly for manufacturing full line of welded and seamless steel pipe, steel tube and tubular products in large diameter.

The main grade of pipeline steel plate are :

Material #: 1.0457, 1.0484, 1.0582, 1.8972, 1.0418, 1.0429, 1.0578, 1.8973, 1.8975, 1.8977, 1.8978

EN 10208-2: L 245NB, L 290NB, L 360NB, L 415NB, L 245MB, L 290MB, L 360MB, L 415MB, L 450MB, L 485MB, L 555MB

DIN 17172: StE 240.7, StE 290.7, StE 360.7, StE 415.7, StE 240.7 TM, StE 290.7 TM, StE 360.7 TM, StE 415.7 TM, StE 445.7 TM, StE 480.7 TM

API 5L : Gr. B, X 42, X 52, X 60, X 65, X 70, X 80.

Steel for large diameter pipes equivalent grades 

	Material #
	EN 10208-2
	DIN 17172
	NFA
	UNI
	BS
	UNE
	API 5L
	JIS

	1.0457
	L 245NB
	StE 240.7
	 
	 
	 
	 
	Gr. B
	 

	1.0484
	L 290NB
	StE 290.7
	 
	 
	 
	 
	X 42
	 

	1.0582
	L 360NB
	StE 360.7
	 
	 
	 
	 
	X 52
	 

	1.8972
	L 415NB
	StE 415.7
	 
	 
	 
	 
	X 60
	 

	1.0418
	L 245MB
	StE 240.7 TM
	 
	 
	 
	 
	Gr. B
	 

	1.0429
	L 290MB
	StE 290.7 TM
	 
	 
	 
	 
	X 42
	 

	1.0578
	L 360MB
	StE 360.7 TM
	 
	 
	 
	 
	X 52
	 

	1.8973
	L 415MB
	StE 415.7 TM
	 
	 
	 
	 
	X 60
	 

	1.8975
	L 450MB
	StE 445.7 TM
	 
	 
	 
	 
	X 65
	 

	1.8977
	L 485MB
	StE 480.7 TM
	 
	 
	 
	 
	X 70
	 

	1.8978
	L 555MB
	 
	 
	 
	 
	 
	X 80
	 


Steel for large diameter pipes Supply Size

Thickness: 8mm to 200mm

Width: 1500mm to 4200mm

Length: 4000mm to 18000mm

Steel for large diameter pipes Delivery state

Hot Rolled, Cold Rolled, Normalized, Quenched, Tempering, Thermal Mechanical Control Process (TMCP), Electroslag Remelting Technical, HIC test.

Steel for large diameter pipes Services

Cutting, Painting, shot blast, and The third party inspection in DNV, BV, LR, GL, ABS, CCS , SGS, and others in super thick ship steel plate.

Bebon International is a global steel supply and stockholding company. Partnerships integrating the resources of the China’s most technically advanced steel mills enable Bebon International to provide a single competitive source for the distribution of steel products worldwide. 

Bebon International offer premium quality Steel for large diameter pipes Plates. These Steel for large diameter pipes plates have consistent and controlled properties, designed for withstanding the high tension for large diameter pipes.

Bebon International has one of the widest steel plate product ranges in the world. Whether you are a designer, contractor or fabricator you will find our product range both modern and extensive. Steel for large diameter pipes offered by Bebon is in very high quality to support the requirements of those engaged in large projects.

[image: image2.jpg]


Bebon steel  ——  The most professional exporter on weathering resistant steel
Tel:0086-371-86151527                                         E-mail:bb@bebonchina.com                           

Fax: 0086-371-86011881                                        MSN:bebonchina@hotmail.com                                 Skype：bebonchina                                             Web:http://www.shipbuilding-steel.com

                                                               http://www.bebonchina.com 

Oficina Dir: 2801 B# Intermational enteprise center Zhengzhou city in China.

