[image: image1.jpg]BEBON

BebonChina.com

3




[image: image1.jpg]                                      Henan BEBON international co.,ltd

Steel pipe and tube

Generally speaking, steel pipe is divided into seamless steel pipe and welded steel pipe . According to the application, there is many type stainless steel pipe, eg: for pipe line, for pressure vessels, for liquid conveyance and so on. About the welded steel pipe, there are:  Longitudinal Submerged Arc Welded Steel Pipe (SAWL steel pipe ), Spiral Submerged Arc Welded Steel Pipe (SSAW steel pipe ), High Frequency Longitudinal Resistance Welded steel pipe  (ERW steel pipe ) and square and rectangular steel pipe .

Bebon international have a professional sales team in steel pipe. Our advantage is seamless steel pipe for pipe line and for liquid conveyance. The main product in this type steel are API 5L ASTM A53 OR ASTM A106 GRA,GRB, X48,X52. The out Diameter is from 3” to 48”, wall thickness from 10SCH to100SCH. The length are Random length, Fixed Length, SRL, DRL. 

Following are specification of seamless steel pipe for line pipe

	Standard
	Steel grade
	Chemical composition %

	
	
	C max
	Mn max
	P max
	S max
	Si
	V
	Nb
	Ti
	CEpcm max

	API 5L  PSL1
	L210 or A
	0.22
	0.90
	0.030
	0.030
	-
	-
	-
	-
	0.25

	
	L245 or B
	0.28
	1.20
	0.030
	0.030
	-
	-
	-
	-
	0.25

	
	L290 or X42
	0.28
	1.30
	0.030
	0.030
	-
	-
	-
	-
	0.25

	
	L320 pr X46
	0.28
	1.40
	0.030
	0.030
	-
	-
	-
	-
	0.25

	
	L360 or X52
	0.28
	1.40
	0.030
	0.030
	-
	-
	-
	-
	0.25

	
	L390 or X56
	0.28
	1.40
	0.030
	0.030
	-
	-
	-
	-
	0.25

	
	L415 or X60
	0.28
	1.40
	0.030
	0.030
	-
	-
	-
	-
	0.25


API 5L seamless steel pipe Mechanical properties
	Standard
	Steel grade
	Yiled strength (min)
	Tensile strength (min)

	API 5LPSL1
	L210 or A
	210
	335

	
	L245 or B
	245
	415

	
	L290 or X42
	290
	415

	
	L320 pr X46
	320
	435

	
	L360 or X52
	360
	460

	
	L390 or X56
	390
	490

	
	L415 or X60
	415
	520


Specification of seamless line for liquid conveyance

	Standard
	Grade
	Chemical composition %

	
	
	C max
	Mn max
	P max
	S max
	Si max
	Cu max
	Ni max
	Mo max
	V max

	DIN
	ST35
	0.18
	0.35-0.65
	0.035
	0.035
	0.15-0.35
	0.25
	0.25
	-
	-

	
	ST45
	0.25
	0.50-0.80
	0.035
	0.035
	0.15-0.35
	0.25
	0.25
	-
	-

	
	ST55
	0.33-0.41
	0.50-0.80
	0.035
	0.035
	0.15-0.35
	0.25
	0.25
	-
	-

	
	ST52
	0.20
	1.50
	0.035
	0.035
	0.55
	0.25
	0.25
	-
	-

	ASTM A53
	A
	0.25
	0.95
	0.05
	0.045
	-
	0.40
	0.40
	0.15
	0.08

	
	B
	0.30
	1.20
	0.05
	0.045
	-
	0.40
	0.40
	0.15
	0.08

	ASTM A106
	A
	0.25
	0.27-0.93
	0.035
	0.035
	0.10
	0.40
	0.40
	0.15
	0.08

	
	B
	0.30
	0.29-1.06
	0.035
	0.035
	0.10
	0.40
	0.40
	0.15
	0.08


 API 5L seamless steel pipe Mechanical properties 
	Standard
	Steel grade
	Yiled strength (min) Mpa
	Tensile strength (min) Mpa
	Elongation% min

	DIN
	ST35
	225
	345-460
	25

	
	ST45
	245
	440-550
	21

	
	ST55
	290
	540-645
	14

	
	ST52
	355
	490-630
	17

	ASTM A53
	A
	205
	330
	22

	
	B
	240
	415
	20

	ASTM A106
	A
	205
	330
	35(longitudinal)

	
	B
	240
	415
	30(longitudinal)


[image: image2.jpg]


Bebon steel  ——  The most professional exporter on weathering resistant steel
Tel:0086-371-86151527                                         E-mail:bb@bebonchina.com                           

Fax: 0086-371-86011881                                        MSN:bebonchina@hotmail.com                                 Skype：bebonchina                                             Web:http://www.shipbuilding-steel.com

                                                               http://www.bebonchina.com 

Oficina Dir: 2801 B# Intermational enteprise center Zhengzhou city in China.

