[image: image1.png]


Henan BEBON international co.,ltd.

 Under  EN10111 standard, MATERIAL# 1.0491 TStE285 steel plate/sheetMain Application:Used in manufacturing shiphull, maritime oil extraction drilling platform, platform tube junction and other structural components.

	S275NL
 EN 10111 MATERIAL# 1.0491
	Comparison of steel grades

	
	UNE36081
	AE 285 KT

	
	DIN17102
	T StE 285

	
	UN
	Fe E 275 KT N

	
	BS4360
	43 EE



 TStE285 steel plate/sheet  Chemical analysis -% by mass*

	Chemical elements
	C
max
	Si
 max
	Mn
max
	P
max
	S
max.
	Cu
max
	Cr
max
	Ni
max
	V
max
	Nb
max
	Al
min

	%,by mass
	0.16
	0.40
	0.50-1.50
	0.025
	0.020
	0.55
	0.30
	0.30
	0.05
	0.05
	0.02



TStE285 steel plate/sheet  Mechanical properties
	thickness
	Yield StrengthReH[N/mm2]
transv.min.
	TensileStrengthRm[N/mm2]transv.
	Fracture Elongation[%]transv. min.
	Notch Impact
Energy1)Ch Vcomplete samplelongitud. min [J]

	t≤ 16mm
t >16mm
	275
265
	 
	 
	         +20   KV 40J
           0   KV 34J
         -10    KV 30J
         -20    KV 27J
         -30    KV 23J
         -40    KV 20J
         -50    KV 16J

	   t < 3mm
  t≥ 3mm
	 
	370-510
	 
	

	Up to 1.5mm
1.51-2.00mm
2.01-2.50mm
2.51-2.99mm
 ≥ 3mm
	 
	 
	24
	


 [image: image3.jpg]


 

[image: image2.jpg]BEBON

BebonChina.com

3




BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


