[image: image1.png]


Henan BEBON international co.,ltd.

 Under  EN10111 standard, S355NL steel plateMain Application:Used in manufacturing shiphull, maritime oil extraction drilling platform, platform tube junction and other structural components.

	S355NL
 EN 10111 MATERIAL# 1.0456
	Comparison of steel grades

	
	UNE36081
	AE 355 KT

	
	DIN17102
	T StE 355

	
	UN
	Fe E 355 KT N

	
	NFA36 201
	E355FP

	
	BS4360
	50 EE



S355NL Chemical analysis -% by mass*

	Chemical elements
	C
max
	Si
 max
	Mn
max
	P
max
	S
max.
	Cu
max
	Cr
max
	Ni
max
	V
max
	Nb
max
	Al
min

	%,by mass
	0.18
	0.50
	0.90-1.65
	0.025
	0.020
	0.55
	0.30
	0.50
	0.12
	0.05
	0.02



Mechanical properties
	thickness
	Yield StrengthReH[N/mm2]
transv.min.
	TensileStrengthRm[N/mm2]transv.
	Fracture Elongation[%]transv. min.
	Notch Impact
Energy1)Ch Vcomplete samplelongitud. min [J]

	t≤ 16mm
t >16mm
	355
345
	 
	 
	         +20   KV 40J
           0   KV 34J
         -10    KV 30J
         -20    KV 27J
         -30    KV 23J
         -40    KV 20J
         -50    KV 16J

	   t < 3mm
  t≥ 3mm
	 
	470-630
	 
	

	Up to 1.5mm
1.51-2.00mm
2.01-2.50mm
2.51-2.99mm
 ≥ 3mm
	 
	 
	22
	




[image: image4.jpg]


 

[image: image2.png]


 

[image: image3.jpg]BEBON

BebonChina.com

3




BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


