[image: image1.png]


Henan BEBON international co.,ltd.

Under  EN10111 standard, S420NL Steel PlateMain ApplicationsUsed for manufacturing factory buildings, general construction and engineering plants, such as, drilling machine, excavator, tip lorry with electric wheel, mining dump truck, grab, shovel loader, bulldozer, all kinds of cranes, coalmine hydraulic support and other machinery and related structure units. 

	S420NL
 EN 10111MATERIAL# 1.8912
	Comparison of steel grades

	
	UNE36081
	AE 420 KT

	
	DIN17102
	T StE 420

	
	UN
	-

	
	NFA36 201
	E420FP

	
	BS4360
	-



 S420NL steel Chemical analysis -% by mass*

	Chemical elements
	C
max
	Si
 max
	Mn
max
	P
max
	S
max.
	Cu
max
	Cr
max
	Ni
max
	V
max
	Nb
max
	Al
min

	%,by mass
	0.20
	0.60
	1.00-1.70
	0.025
	0.020
	0.55
	0.30
	0.80
	0.20
	0.05
	0.02



S420NL  Alloy steel Mechanical properties
	thickness
	Yield StrengthReH[N/mm2]
transv.min.
	TensileStrengthRm[N/mm2]transv.
	Fracture Elongation[%]transv. min.
	Notch Impact
Energy1)Ch Vcomplete samplelongitud. min [J]

	t≤ 16mm
t >16mm
	420
400
	 
	 
	         +20   KV 40J
           0   KV 34J
         -10    KV 30J
         -20    KV 27J
         -30    KV 23J
         -40    KV 20J
         -50    KV 16J

	   t < 3mm
  t≥ 3mm
	 
	520-680
	 
	

	Up to 1.5mm
1.51-2.00mm
2.01-2.50mm
2.51-2.99mm
 ≥ 3mm
	 
	 
	19
	


[image: image3.jpg]


 

[image: image2.jpg]BEBON

BebonChina.com

3




BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


