[image: image1.jpg]BEBON

BebonChina.com

3




Henan BEBON international co.,ltd.

Under EN10025-3 standard,S460NL steel Makes mechanical device and other structural elements like drilling machine, power shovel, electricity drive wheel counter- mine trolley, mineral product automobile, excavator, car loader, bulldozer, each kind of hoist crane, coal mine hydraulic pressure support which were widely used in workshop, the general construction and each kind of project machinery, like the mine and each kind of project construction.

	S460NL
 EN 10025-3
	Comparison of steel grades

	
	UNE36081
	AE 460 KT

	
	DIN17102
	T StE 460

	
	UN
	FE E 460KT N

	
	NFA36 201
	E460FP

	
	BS4360
	55EE




 S460NL steel plate Chemical analysis -% by mass*

	Chemical elements
	C

max
	Si
max
	Mn
max
	P
max
	S
max.
	Cu

max
	Cr

max
	Ni

max
	V

max
	Nb

max
	Al

min

	%,by mass
	0.20
	0.60
	1.00-1.70
	0.025
	0.020
	0.55
	0.30
	0.80
	0.20
	0.05
	0.02



S460NL steel sheet Mechanical properties
	thickness
	Yield StrengthReH[N/mm2]
transv.min.
	TensileStrengthRm[N/mm2]transv.
	Fracture Elongation[%]transv. min.
	Notch Impact
Energy1)Ch Vcomplete samplelongitud. min [J]

	t≤ 16mm

t >16mm
	460
440
	 
	 
	         +20   KV 40J

           0   KV 34J

         -10    KV 30J

         -20    KV 27J

         -30    KV 23J

         -40    KV 20J

         -50    KV 16J

	   t < 3mm

  t ≥ 3mm
	 
	540-720
	 
	

	Up to 1.5mm

1.51-2.00mm

2.01-2.50mm

2.51-2.99mm

 ≥ 3mm
	 
	 
	17
	


[image: image2.jpg]


BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


