| 18CrNiMo7-6 EN 10084-1998, Number: 1.6587 | Comparison of steel grades |  |
| --- | --- | --- |
|  | JUS | Ć.4520 |
|  | DIN | 17CrNiMo6 |
|  | BS | - |
|  | GOST | - |
|  | AISI | 4820 |
|  | UNI | - |
|  | NF | 18NCD6 |

Chemical composition (cast analysis)

| Chemical elements | C | Si max | Mn | P max. | S | Cr | Mo | Ni |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| %, by mass | 0,15-0,21 | 0,40 | 0,50-0,90 | 0,035 | ≤ 0,035 | 1,50-1,80 | 0,25-0,35 | 1,40-1,70 |
| Permissible deviation | ± 0,02 | + 0,03 | ± 0,04 | + 0,005 | + 0,005 | ± 0,05 | ± 0,02 | ± 0,02 |

Hardness limits for steel

| Hardness HRC at a distance from quenched end of test piece (in milimetres) of |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| mm |  |  | 1,5 |  | 3 |  | 5 |  | 7 |  | 9 |  | 11 |  | 13 |  | 15 |  | 20 |  | 25 |  | 30 |  | 35 |  | 40 |  | 45 |  | 50 |
| +H | max. | 48 |  | 48 |  | 48 |  | 48 |  | 47 |  | 47 |  | 46 |  | 46 |  | 44 |  | 43 |  | 42 |  | 41 |  | 41 |  | - |  | - |  |
|  | min. | 40 |  | 40 |  | 39 |  | 38 |  | 37 |  | 36 |  | 35 |  | 34 |  | 32 |  | 31 |  | 30 |  | 29 |  | 29 |  | - |  | - |  |
| +HH | max. | 48 |  | 48 |  | 48 |  | 48 |  | 47 |  | 47 |  | 46 |  | 46 |  | 44 |  | 43 |  | 42 |  | 41 |  | 41 |  | - |  | - |  |
|  | min. | 43 |  | 43 |  | 42 |  | 41 |  | 40 |  | 40 |  | 39 |  | 38 |  | 36 |  | 35 |  | 34 |  | 33 |  | 33 |  | - |  | - |  |
| +HL | max. | 45 |  | 45 |  | 45 |  | 45 |  | 44 |  | 43 |  | 42 |  | 42 |  | 40 |  | 39 |  | 38 |  | 37 |  | 37 |  | - |  | - |  |
|  | min. | 40 |  | 40 |  | 39 |  | 38 |  | 37 |  | 36 |  | 35 |  | 34 |  | 32 |  | 31 |  | 30 |  | 29 |  | 29 |  | - |  | - |  |

Hardness requirements for products delivered in the conditions ’’treated to improve shearabilita’’ (+S), ’’anneled to maximum hardness requirements’’ (+A), ’’treated to hardness range’’ (+TH) or ’’treated to ferrite-pearlite structure and hardness range’’ (+FP)

| Brinell hardness in the condition |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| +S max. | +A max. | +TH |  |  |  | +FP |  |  |
|  |  | min. |  | max. | min. |  | max. |  |
| 255 | 229 | 179 | 229 |  |  | 159 |  | 207 |

Non-metallic inclusions Requirements for microscopic degree of purity when tested in accordance with DIN 50 602 (method K) (valid for oxidic non-metallic inclusions)

| D (mm) Bars Diameter d (mm) | K Total characteristic value K (oxides) for the individual cast |
| --- | --- |
| 140 < d 200 | K 4 ≤ 50 |
| 100 < d ≤ 140 | K 4 ≤ 45 |
| 70 < d ≤ 100 | K 4 ≤ 40 |
| 35 < d ≤ 70 | K 4 ≤ 35 |
| 17 < d ≤ 35 | K 3 ≤ 40 |
| 8 < d ≤ 17 | K 3 ≤ 30 |
| d ≤ 8 | K 2≤ 35 |

Conditions for heat treating test bars and treatment of the steels

| End quenchh test Quenching, 0C | Carbunnzing temperature, 0C | Core-hardening temperature, 0C | Case-hardening temperature, 0C | Tempering, 0C |
| --- | --- | --- | --- | --- |
| 860 | 880 to 980 | 830 to 870 | 780 to 820 | 150 to 200 |